Virginia Department of Historical Resources

Conservation Laboratory

T - R - E - A - T - M - E - N - T    R - E - C - O - R - D

LAB # 55

Date	                Treatment Action

1) 2/3/92		Examination -- magnification -- solid core but

calcareous deposit on exterior.

EDTA, low heat - removed calcareous deposit and

CuCO3.   Cu ring, NO ENGRAVING.

Demineralized H20 soak.

Acetone rinse.

2/4/92	Incralac 6.5%/Toluene solution vacuum impregnation                 at 20 psi for one hour.

Air dry/blower.

Repackage/ziplock.

2/19/92	PHOTO KPA Color Slide Film AFTER TREATMENT

2)   1/31/92	Examination -- magnification.

Mechanical cleaning - steel instruments - no 			evidence of plating on Cu inlay, but rivets do

exhibit small tin plate areas.

Acetone clean/swab.

Incralac 6.5%/Toluene solution - 2 brush coats on

Cu inlay and rivets only.

Renaissance wax on jet.

Repackage/ziplock.

2/19/92	PHOTO KPA Color Slide Film AFTER TREATMENT