Virginia Department of Historical Resources

Conservation Laboratory

T - R - E - A - T - M - E - N - T    R - E - C - O - R - D

LAB # 306

Date	                Treatment Action

1)  6/8/92		Examination -- magnification.

Mechanical cleaning/EtOH rinse.

Rinse w/3% Orvus and DI H2O at room temp.

Soak sandwich in 10% Glycerin/.5% Ethulose/

DI H2O for one week.

6/23/92	H20 rinse/warm.

Demineralized H20 rinse.

Dry under weights - ethafoam/kimwipe - sandwich.

6/26/92	Examination -- magnification 20x -- approximately

8 frags.  Loose weave with nap, easily matted,

yellow/brown.

Materials testing - burn = ash, "burning hair" odor

WOOL.  Most frags exhibit irrigular edge, one

may have a selvage edge.  Extreme matting and

frequent distortion of very loose weave.

2)  6/23/92	Examination -- visual.

EtOH & brush.  Air dry/blower.

7/8/92		Incralac 6.5%/Toluene solution - 2 brush coats -

Cu alloy snap area only.

Air dry/screen.

Repackage/ziplock.

ALL 7/20/92	PHOTO EC-100 Color Slide Film  AFTER TREATMENT